## Slide 1: Memory Systems and Memory-Centric Computing Systems Topic 2: Memory Reliability and Security
Prof. Onur Mutlu
omutlu@gmail.com
https://people.inf.ethz.ch/omutlu
9-13 July 2018
HiPEAC ACACES Summer School 2018

## Slide 2: What Will You Learn in This Course?
Memory Systems and Memory-Centric Computing Systems
  July 9-13, 2018
Topic 1: Main Memory Trends and Basics
Topic 2: Memory Reliability & Security: RowHammer and Beyond
Topic 3: In-memory Computation
Topic 4: Low-Latency and Low-Energy Memory
Topic 5 (unlikely): Enabling and Exploiting Non-Volatile Memory
Topic 6 (unlikely): Flash Memory and SSD Scaling
Major Overview Reading:
  Mutlu and Subramaniam, “Research Problems and Opportunities in Memory Systems,” SUPERFRI 2014.

## Slide 3: Agenda
Brief Introduction
A Motivating Example
Memory System Trends
What Will You Learn In This Course
  And, how to make the best of it…
Memory Fundamentals
Key Memory Challenges and Solution Directions
  Security, Reliability, Safety
  Energy and Performance: Data-Centric Systems
  Latency and Latency-Reliability Tradeoffs
Summary and Future Lookout

## Slide 4: Four Key Directions
Fundamentally Secure/Reliable/Safe Architectures
Fundamentally Energy-Efficient Architectures
  Memory-centric (Data-centric) Architectures
Fundamentally Low-Latency Architectures
Architectures for Genomics, Medicine, Health

## Slide 5: Maslow’s (Human) Hierarchy of Needs
We need to start with reliability and security…
Maslow, “A Theory of Human Motivation,”
Psychological Review, 1943.
Source: https://www.simplypsychology.org/maslow.html
Maslow, “A Theory of Human Motivation,”
Psychological Review, 1943.
Maslow, “Motivation and Personality,”
Book, 1954-1970.

## Slide 6: How Reliable/Secure/Safe is This Bridge?
Source: http://www.technologystudent.com/struct1/tacom1.png

## Slide 7: Collapse of the “Galloping Gertie”
Source: AP

## Slide 8: How Secure Are These People?
Source: https://s-media-cache-ak0.pinimg.com/originals/48/09/54/4809543a9c7700246a0cf8acdae27abf.jpg
Security is about preventing unforeseen consequences

## Slide 9: The DRAM Scaling Problem
DRAM stores charge in a capacitor (charge-based memory)
  Capacitor must be large enough for reliable sensing
  Access transistor should be large enough for low leakage and high retention time
  Scaling beyond 40-35nm (2013) is challenging [ITRS, 2009]
DRAM capacity, cost, and energy/power hard to scale

## Slide 10: As Memory Scales, It Becomes Unreliable
Data from all of Facebook’s servers worldwide
Meza+, “Revisiting Memory Errors in Large-Scale Production Data Centers,” DSN’15.
Intuition: quadratic increase in capacity

## Slide 11: Large-Scale Failure Analysis of DRAM Chips
Analysis and modeling of memory errors found in all of Facebook’s server fleet
Justin Meza, Qiang Wu, Sanjeev Kumar, and Onur Mutlu, "Revisiting Memory Errors in Large-Scale Production Data Centers: Analysis and Modeling of New Trends from the Field" Proceedings of the 45th Annual IEEE/IFIP International Conference on Dependable Systems and Networks (DSN), Rio de Janeiro, Brazil, June 2015. [Slides (pptx) (pdf)] [DRAM Error Model]

## Slide 12: Infrastructures to Understand Such Issues
  An Experimental Study of Data Retention Behavior in Modern DRAM Devices: Implications for Retention Time Profiling Mechanisms (Liu et al., ISCA 2013)
  The Efficacy of Error Mitigation Techniques for DRAM Retention Failures: A Comparative Experimental Study
  (Khan et al., SIGMETRICS 2014)
  Flipping Bits in Memory Without Accessing Them: An Experimental Study of DRAM Disturbance Errors (Kim et al., ISCA 2014)
  Adaptive-Latency DRAM: Optimizing DRAM Timing for the Common-Case (Lee et al., HPCA 2015)
  AVATAR: A Variable-Retention-Time (VRT) Aware Refresh for DRAM Systems (Qureshi et al., DSN 2015)

## Slide 13: Infrastructures to Understand Such Issues
  Kim+, “Flipping Bits in Memory Without Accessing Them: An Experimental Study of DRAM Disturbance Errors,” ISCA 2014.
Temperature
Controller
PC
Heater
FPGAs
FPGAs

## Slide 14: SoftMC: Open Source DRAM Infrastructure
Hasan Hassan et al., “SoftMC: A Flexible and Practical Open-Source Infrastructure for Enabling Experimental DRAM Studies,” HPCA 2017.
Flexible
Easy to Use (C++ API)
Open-source
github.com/CMU-SAFARI/SoftMC

## Slide 15: SoftMC
https://github.com/CMU-SAFARI/SoftMC

## Slide 16: Data Retention in Memory [Liu et al., ISCA 2013]
Retention Time Profile of DRAM looks like this:
Location dependent
Stored value pattern dependent
Time dependent

## Slide 17: A Curious Discovery [Kim et al., ISCA 2014]
One can
predictably induce errors
in most DRAM memory chips

## Slide 18: DRAM RowHammer
A simple hardware failure mechanism
can create a widespread
system security vulnerability

## Slide 19: Modern DRAM is Prone to Disturbance Errors
Row of Cells
Row
Row
Row
Row
Wordline
VLOW
VHIGH
Victim Row
Victim Row
Hammered Row
Repeatedly reading a row enough times (before memory gets refreshed) induces disturbance errors in adjacent rows in most real DRAM chips you can buy today
Opened
Closed
Flipping Bits in Memory Without Accessing Them: An Experimental Study of DRAM Disturbance Errors, (Kim et al., ISCA 2014)

## Slide 20: Most DRAM Modules Are Vulnerable
86%
(37/43)
83%
(45/54)
88%
(28/32)
A company
B company
C company
Up to
1.0×107 errors
Up to
2.7×106 errors
Up to
3.3×105 errors
Flipping Bits in Memory Without Accessing Them: An Experimental Study of DRAM Disturbance Errors, (Kim et al., ISCA 2014)

## Slide 21: Recent DRAM Is More Vulnerable
Notes: In this figure, the x-axis is the module manufacture date. And the y-axis is the number of errors in a module, normalized to one billion cells. In 2008 and 2009, there are no errors. But, in 2010, we first start to see errors in C modules. After 2010, the errors start to proliferate. For A and B modules, we first start to see errors in 2011. In particular, all modules from 2012 and 2013 are vulnerable.

## Slide 22: Recent DRAM Is More Vulnerable
First
Appearance
Notes: In this figure, the x-axis is the module manufacture date. And the y-axis is the number of errors in a module, normalized to one billion cells. In 2008 and 2009, there are no errors. But, in 2010, we first start to see errors in C modules. After 2010, the errors start to proliferate. For A and B modules, we first start to see errors in 2011. In particular, all modules from 2012 and 2013 are vulnerable.

## Slide 23: Recent DRAM Is More Vulnerable
All modules from 2012–2013 are vulnerable
First
Appearance
Notes: In this figure, the x-axis is the module manufacture date. And the y-axis is the number of errors in a module, normalized to one billion cells. In 2008 and 2009, there are no errors. But, in 2010, we first start to see errors in C modules. After 2010, the errors start to proliferate. For A and B modules, we first start to see errors in 2011. In particular, all modules from 2012 and 2013 are vulnerable.

## Slide 24: A Simple Program Can Induce Many Errors
CPU
loop:
mov (X), %eax
mov (Y), %ebx
clflush (X)
clflush (Y)
mfence
jmp loop
  Download from: https://github.com/CMU-SAFARI/rowhammer
DRAM Module
Y
X
Notes: We demonstrate the errors on multiple x86 systems. Shown to the bottom-left is a “disturbance kernel”. When executed, it forces two rows to be opened and closed one after the other – over and over again. Consequently, it induces many errors in the module.

## Slide 25: A Simple Program Can Induce Many Errors
CPU
  Download from: https://github.com/CMU-SAFARI/rowhammer
DRAM Module
Y
X
Avoid cache hits
  Flush X from cache
Avoid row hits to X
  Read Y in another row
Notes: We demonstrate the errors on multiple x86 systems. Shown to the bottom-left is a “disturbance kernel”. When executed, it forces two rows to be opened and closed one after the other – over and over again. Consequently, it induces many errors in the module.

## Slide 26: A Simple Program Can Induce Many Errors
CPU
loop:
mov (X), %eax
mov (Y), %ebx
clflush (X)
clflush (Y)
mfence
jmp loop
  Download from: https://github.com/CMU-SAFARI/rowhammer
DRAM Module
Y
X
Notes: We demonstrate the errors on multiple x86 systems. Shown to the bottom-left is a “disturbance kernel”. When executed, it forces two rows to be opened and closed one after the other – over and over again. Consequently, it induces many errors in the module.

## Slide 27: A Simple Program Can Induce Many Errors
CPU
loop:
mov (X), %eax
mov (Y), %ebx
clflush (X)
clflush (Y)
mfence
jmp loop
  Download from: https://github.com/CMU-SAFARI/rowhammer
DRAM Module
Y
X
Notes: We demonstrate the errors on multiple x86 systems. Shown to the bottom-left is a “disturbance kernel”. When executed, it forces two rows to be opened and closed one after the other – over and over again. Consequently, it induces many errors in the module.

## Slide 28: A Simple Program Can Induce Many Errors
CPU
loop:
mov (X), %eax
mov (Y), %ebx
clflush (X)
clflush (Y)
mfence
jmp loop
Y
X
  Download from: https://github.com/CMU-SAFARI/rowhammer
DRAM Module
Notes: We demonstrate the errors on multiple x86 systems. Shown to the bottom-left is a “disturbance kernel”. When executed, it forces two rows to be opened and closed one after the other – over and over again. Consequently, it induces many errors in the module.

## Slide 29: Observed Errors in Real Systems
A real reliability & security issue
CPU Architecture | Errors | Access-Rate
Intel Haswell (2013) | 22.9K | 12.3M/sec
Intel Ivy Bridge (2012) | 20.7K | 11.7M/sec
Intel Sandy Bridge (2011) | 16.1K | 11.6M/sec
AMD Piledriver (2012) | 59 | 6.1M/sec
Kim+, “Flipping Bits in Memory Without Accessing Them: An Experimental Study of DRAM Disturbance Errors,” ISCA 2014.
Notes: When we executed the code on four different processors, all four of them yielded errors. Intel Haswell has the most errors, at 23 thousand, because it has the highest rate of accessing DRAM.
Later on, I’ll show that we can induce as many as ten million disturbance errors in a more controlled environment.
From this, we conclude that disturbance errors are a serious reliability issue.

## Slide 30: One Can Take Over an Otherwise-Secure System
Exploiting the DRAM rowhammer bug to gain kernel privileges (Seaborn, 2015)
Flipping Bits in Memory Without Accessing Them: An Experimental Study of DRAM Disturbance Errors (Kim et al., ISCA 2014)

## Slide 31: RowHammer Security Attack Example
“Rowhammer” is a problem with some recent DRAM devices in which repeatedly accessing a row of memory can cause bit flips in adjacent rows (Kim et al., ISCA 2014).
  Flipping Bits in Memory Without Accessing Them: An Experimental Study of DRAM Disturbance Errors (Kim et al., ISCA 2014)
We tested a selection of laptops and found that a subset of them exhibited the problem.
We built two working privilege escalation exploits that use this effect.
  Exploiting the DRAM rowhammer bug to gain kernel privileges (Seaborn+, 2015)
One exploit uses rowhammer-induced bit flips to gain kernel privileges on x86-64 Linux when run as an unprivileged userland process.
When run on a machine vulnerable to the rowhammer problem, the process was able to induce bit flips in page table entries (PTEs).
It was able to use this to gain write access to its own page table, and hence gain read-write access to all of physical memory.
Exploiting the DRAM rowhammer bug to gain kernel privileges (Seaborn & Dullien, 2015)

## Slide 32: Security Implications
Notes: Picture from the article:
http://thehackernews.com/2015/03/dram-rowhammer-vulnerability.html

## Slide 33: Security Implications
Notes: Picture from the article:
http://thehackernews.com/2015/03/dram-rowhammer-vulnerability.html

## Slide 34: Selected Readings on RowHammer (I)
Our first detailed study: Rowhammer analysis and solutions (June 2014)
  Yoongu Kim, Ross Daly, Jeremie Kim, Chris Fallin, Ji Hye Lee, Donghyuk Lee, Chris Wilkerson, Konrad Lai, and Onur Mutlu, "Flipping Bits in Memory Without Accessing Them: An Experimental Study of DRAM Disturbance Errors" Proceedings of the 41st International Symposium on Computer Architecture (ISCA), Minneapolis, MN, June 2014. [Slides (pptx) (pdf)] [Lightning Session Slides (pptx) (pdf)] [Source Code and Data]
Our Source Code to Induce Errors in Modern DRAM Chips (June 2014)
  https://github.com/CMU-SAFARI/rowhammer
Google Project Zero’s Attack to Take Over a System (March 2015)
  Exploiting the DRAM rowhammer bug to gain kernel privileges (Seaborn+, 2015)
  https://github.com/google/rowhammer-test
  Double-sided Rowhammer

## Slide 35: Selected Readings on RowHammer (II)
Remote RowHammer Attacks via JavaScript (July 2015)
  http://arxiv.org/abs/1507.06955
  https://github.com/IAIK/rowhammerjs
  Gruss et al., DIMVA 2016.
  CLFLUSH-free Rowhammer
  “A fully automated attack that requires nothing but a website with JavaScript to trigger faults on remote hardware.”
  “We can gain unrestricted access to systems of website visitors.”
ANVIL: Software-Based Protection Against Next-Generation Rowhammer Attacks (March 2016)
  http://dl.acm.org/citation.cfm?doid=2872362.2872390
  Aweke et al., ASPLOS 2016
  CLFLUSH-free Rowhammer
  Software based monitoring for rowhammer detection

## Slide 36: Selected Readings on RowHammer (III)
Dedup Est Machina: Memory Deduplication as an Advanced Exploitation Vector (May 2016)
  https://www.ieee-security.org/TC/SP2016/papers/0824a987.pdf
  Bosman et al., IEEE S&P 2016.
  Exploits Rowhammer and Memory Deduplication to overtake a browser
  “We report on the first reliable remote exploit for the Rowhammer vulnerability running entirely in Microsoft Edge.”
  “[an attacker] … can reliably “own” a system with all defenses up, even if the software is entirely free of bugs.”

## Slide 37: Selected Readings on RowHammer (IV)
Flip Feng Shui: Hammering a Needle in the Software Stack (August 2016)
  https://www.usenix.org/system/files/conference/usenixsecurity16/sec16_paper_razavi.pdf
  Razavi et al., USENIX Security 2016.
  Combines memory deduplication and RowHammer
  “A malicious VM can gain unauthorized access to a co-hosted VM running OpenSSH.”
  Breaks OpenSSH public key authentication
Drammer: Deterministic Rowhammer Attacks on Mobile Platforms (October 2016)
  http://dl.acm.org/citation.cfm?id=2976749.2978406
  Van Der Veen et al., CCS 2016
  Can take over an ARM-based Android system deterministically
  Exploits predictable physical memory allocator behavior
    Can deterministically place security-sensitive data (e.g., page table) in an attacker-chosen, vulnerable location in memory

## Slide 38: Selected Readings on RowHammer (V)
Grand Pwning Unit: Accelerating Microarchitectural Attacks with the GPU (May 2018)
  https://www.vusec.net/wp-content/uploads/2018/05/glitch.pdf
  Frigo et al., IEEE S&P 2018.
  The first end-to-end remote Rowhammer exploit on mobile platforms that use our GPU-based primitives in orchestration to compromise browsers on mobile devices in under two minutes.
Throwhammer: Rowhammer Attacks over the Network and Defenses (July 2018)
  https://www.cs.vu.nl/~herbertb/download/papers/throwhammer_atc18.pdf
  Tatar et al., USENIX ATC 2018.
  “[We] show that an attacker can trigger and exploit Rowhammer bit flips directly from a remote machine by only sending network packets.”

## Slide 39: Selected Readings on RowHammer (VI)
Nethammer: Inducing Rowhammer Faults through Network Requests (July 2018)
  https://arxiv.org/pdf/1805.04956.pdf
  Lipp et al., arxiv.org 2018.
  “Nethammer is the first truly remote Rowhammer attack, without a single attacker-controlled line of code on the targeted system.”

## Slide 40: More Security Implications (I)
Source: https://lab.dsst.io/32c3-slides/7197.html
Rowhammer.js: A Remote Software-Induced Fault Attack in JavaScript (DIMVA’16)
“We can gain unrestricted access to systems of website visitors.”

## Slide 41: More Security Implications (II)
Source: https://fossbytes.com/drammer-rowhammer-attack-android-root-devices/
Drammer: Deterministic Rowhammer Attacks on Mobile Platforms, CCS’16
  “Can gain control of a smart phone deterministically”

## Slide 42: More Security Implications (III)
Using an integrated GPU in a mobile system to remotely escalate privilege via the WebGL interface

## Slide 43: More Security Implications (IV)
Rowhammer over RDMA (I)

## Slide 44: More Security Implications (V)
Rowhammer over RDMA (II)

## Slide 45: More Security Implications?

## Slide 46: RowHammer Solutions

## Slide 47: Some Potential Solutions
Cost
Make better DRAM chips
Cost, Power
Sophisticated ECC
Power, Performance
Refresh frequently
Cost, Power, Complexity
Access counters
Notes: Here is a list of four potential solutions to disturbance errors: making better DRAM chips, refreshing more frequently, employing sophisticated ECC schemes, and using hardware counters to track the number of accesses to different rows.
However, all of these solutions incur a large overhead in terms cost, power, performance, and/or complexity.

## Slide 48: Naive Solutions
❶ Throttle accesses to same row
  Limit access-interval: ≥500ns
  Limit number of accesses: ≤128K (=64ms/500ns)
❷ Refresh more frequently
  Shorten refresh-interval by ~7x
Both naive solutions introduce significant overhead in performance and power
Notes: Based on what we learned from the sensitivity studies, there are two naive solutions that immediately present themselves.
First, we can throttle accesses to the same row. If the access-interval is greater than 500ns, I showed how errors are not induced. We can achieve the same effect by limiting the maximum number of accesses to the same row to be less than 128K, within a refresh interval.
Second, we can refresh the module more frequently. If the refresh-interval is shortened by 7x, I showed how errors can be prevented.
However, both naive solutions introduce significant overhead in both performance and power. Later on, I will propose a much more efficient solution.

## Slide 49: Apple’s Patch for RowHammer
https://support.apple.com/en-gb/HT204934
HP, Lenovo, and other vendors released similar patches

## Slide 50: Our Solution to RowHammer
PARA: Probabilistic Adjacent Row Activation
Key Idea
  After closing a row, we activate (i.e., refresh) one of its neighbors with a low probability: p = 0.005
Reliability Guarantee
  When p=0.005, errors in one year: 9.4×10-14
  By adjusting the value of p, we can vary the strength of protection against errors
Notes: We provide a more efficient solution, called PARA, which stands for probabilistic adjacent row activation.
The key idea is thus: after closing a row, we activate (i.e., refresh) one of its neighbors with a low probability, for example, p equal to 0.005.
PARA provides a strong reliability guarantee even under the worst-case access patterns to DRAM. When we set p to 0.005, the expected number of errors in one year is 9.4 times 10 to the negative 14. This probability is much lower the failure rate of other hardware components, for example, the hard-disk drive.
And by adjusting the value of p, PARA can provide an arbitrarily strong-degree of protection against errors.

## Slide 51: Advantages of PARA
PARA refreshes rows infrequently
  Low power
  Low performance-overhead
    Average slowdown: 0.20% (for 29 benchmarks)
    Maximum slowdown: 0.75%
PARA is stateless
  Low cost
  Low complexity
PARA is an effective and low-overhead solution to prevent disturbance errors
Notes: PARA has many advantages. Since it refreshes row infrequently, it has low power and low performance-overhead. Simulated across 29 benchmarks, we saw an average of only 0.2% slowdown and a maximum of only 0.75% slowdown.
In addition, due to its stateless nature, PARA has low cost and complexity.
Therefore, PARA is an effective and low-overhead solution to prevent disturbance errors.

## Slide 52: Requirements for PARA
If implemented in DRAM chip
  Enough slack in timing parameters
  Plenty of slack today:
    Lee et al., “Adaptive-Latency DRAM: Optimizing DRAM Timing for the Common Case,” HPCA 2015.
    Chang et al., “Understanding Latency Variation in Modern DRAM Chips,” SIGMETRICS 2016.
    Lee et al., “Design-Induced Latency Variation in Modern DRAM Chips,” SIGMETRICS 2017.
    Chang et al., “Understanding Reduced-Voltage Operation in Modern DRAM Devices,” SIGMETRICS 2017.
If implemented in memory controller
  Better coordination between memory controller and DRAM
  Memory controller should know which rows are physically adjacent

## Slide 53: More on RowHammer Analysis
Yoongu Kim, Ross Daly, Jeremie Kim, Chris Fallin, Ji Hye Lee, Donghyuk Lee, Chris Wilkerson, Konrad Lai, and Onur Mutlu, "Flipping Bits in Memory Without Accessing Them: An Experimental Study of DRAM Disturbance Errors" Proceedings of the 41st International Symposium on Computer Architecture (ISCA), Minneapolis, MN, June 2014. [Slides (pptx) (pdf)] [Lightning Session Slides (pptx) (pdf)] [Source Code and Data]

## Slide 54: Future of Memory Reliability
https://people.inf.ethz.ch/omutlu/pub/rowhammer-and-other-memory-issues_date17.pdf
Onur Mutlu, "The RowHammer Problem and Other Issues We May Face as Memory Becomes Denser" Invited Paper in Proceedings of the Design, Automation, and Test in Europe Conference (DATE), Lausanne, Switzerland, March 2017. [Slides (pptx) (pdf)]

## Slide 55: Industry Is Writing Papers About It, Too

## Slide 56: Call for Intelligent Memory Controllers

## Slide 57: Aside: Intelligent Controller for NAND Flash
USB Jack
Virtex-II Pro
(USB controller)
Virtex-V FPGA
(NAND Controller)
HAPS-52 Mother Board
USB Daughter Board
NAND Daughter Board
1x-nm
NAND Flash
Cai+, “Error Characterization, Mitigation, and Recovery in Flash Memory Based Solid State Drives,” Proc. IEEE 2017.
[DATE 2012, ICCD 2012, DATE 2013, ITJ 2013, ICCD 2013, SIGMETRICS 2014, HPCA 2015, DSN 2015, MSST 2015, JSAC 2016, HPCA 2017, DFRWS 2017,
PIEEE 2017, HPCA 2018, SIGMETRICS 2018]

## Slide 58: Aside: Intelligent Controller for NAND Flash
https://arxiv.org/pdf/1706.08642
Proceedings of the IEEE, Sept. 2017

## Slide 59: A Key Takeaway
Main Memory Needs
Intelligent Controllers

## Slide 60: Understanding RowHammer

## Slide 61: Root Causes of Disturbance Errors
Cause 1: Electromagnetic coupling
  Toggling the wordline voltage briefly increases the voltage of adjacent wordlines
  Slightly opens adjacent rows  Charge leakage
Cause 2: Conductive bridges
Cause 3: Hot-carrier injection
Confirmed by at least one manufacturer
Notes: Why do the errors occur? We see three possible causes.
First, there could electromagnetic coupling between adjacent wordlines. When the voltage of one is toggled, it could briefly increase the voltage of the other and facilitate the leakage of charge.
Two other possibilities are conductive bridges and hot-carrier injection.
At least one manufacturer confirmed that these three could play a role in the disturbance errors we see them today.

## Slide 62: Experimental DRAM Testing Infrastructure
  An Experimental Study of Data Retention Behavior in Modern DRAM Devices: Implications for Retention Time Profiling Mechanisms (Liu et al., ISCA 2013)
  The Efficacy of Error Mitigation Techniques for DRAM Retention Failures: A Comparative Experimental Study
  (Khan et al., SIGMETRICS 2014)
  Flipping Bits in Memory Without Accessing Them: An Experimental Study of DRAM Disturbance Errors (Kim et al., ISCA 2014)
  Adaptive-Latency DRAM: Optimizing DRAM Timing for the Common-Case (Lee et al., HPCA 2015)
  AVATAR: A Variable-Retention-Time (VRT) Aware Refresh for DRAM Systems (Qureshi et al., DSN 2015)

## Slide 63: Experimental DRAM Testing Infrastructure
  Kim+, “Flipping Bits in Memory Without Accessing Them: An Experimental Study of DRAM Disturbance Errors,” ISCA 2014.
Temperature
Controller
PC
Heater
FPGAs
FPGAs

## Slide 64: RowHammer Characterization Results
Most Modules Are at Risk
Errors vs. Vintage
Error = Charge Loss
Adjacency: Aggressor & Victim
Sensitivity Studies
Other Results in Paper
Solution Space
Flipping Bits in Memory Without Accessing Them: An Experimental Study of DRAM Disturbance Errors, (Kim et al., ISCA 2014)
Notes: Now I will present the characterization results, one-by-one.
First, I show that most modules are at risk. Second, I show the number of errors in a module as a function of the manufacture date. Third, I show that the errors are symptomatic of charge loss. Fourth, I show that an aggressor induces errors in adjacent rows. Fifth, I show several sensitivity studies. And, finally, I briefly describe other results in the paper.

## Slide 65: 4. Adjacency: Aggressor & Victim
Most aggressors & victims are adjacent
Note: For three modules with the most errors (only first bank)
Adjacent
Adjacent
Adjacent
Non-Adjacent
Non-Adjacent
Notes: In this figure, the x-axis is the row-address difference between an aggressor and its victims. And the y-axis is the number of victim-aggressor pairs that correspond to the row-address difference. For all three modules, we see strong peaks at plus/minus 1. This implies that aggressors and victims have consecutive row-addresses, in other words, they are adjacent.
However, the figure also shows some victims that are not adjacent to the aggressor. We believe this could be caused by two reasons. First, depending on the mapping, two rows that are physically adjacent within the DRAM chip may not have consecutive row-addresses. Second, fault rows are often re-mapped to spare rows that may reside on a different portion of the DRAM chip.
Nevertheless, we conclude that the vast majority of aggressors & victims are adjacent.

## Slide 66: ❶ Access Interval (Aggressor)
Note: For three modules with the most errors (only first bank)
Not Allowed
Less frequent accesses  Fewer errors
55ns
500ns
Notes: In this figure, the x-axis is the interval at which we access the aggressor. And the y-axis is the number of errors. To comply with the DRAM standard, we employ a default value of 55ns in our experiments. However, as we increase the access-interval, we see that the number of errors decreases. In particular, at 500ns, there are no errors for all three modules.
From this, we conclude that less frequent accesses induce fewer errors.

## Slide 67: ❷ Refresh Interval
Note: Using three modules with the most errors (only first bank)
More frequent refreshes  Fewer errors
~7x frequent
64ms
Notes: In this figure, the x-axis is the refresh-interval. And the y-axis is the number of errors. To comply with the DRAM standard, we employ a default value of 64ms in our experiments. However, as we decrease the refresh-interval, we see that the number of errors decreases. In particular, when the refresh is shortened by 7x, there are no errors for all three modules.
From this, we conclude that more frequent accesses induce fewer errors.

## Slide 68: ❸ Data Pattern
RowStripe
~RowStripe
111111
111111
111111
111111
000000
000000
000000
000000
000000
111111
000000
111111
111111
000000
111111
000000
Solid
~Solid
10x Errors
Errors affected by data stored in other cells
Notes: We tested the modules with four different data-patterns: Solid, inverse Solid, RowStripe, and inverse RowStripe. Solid and inverse Solid give us full coverage since each cell is tested with both 1s and 0s. And the same applies to RowStripe and its inverse.
However, we found that the rowstripe pattern had 10 times as more errors than the solid pattern. We also tested many other data-patterns, including random, but found RowStripe to induce the most errors.
Therefore, we conclude that errors are affected by data stored in other cells due to differences in coupling effects between the cells.

## Slide 69: 6. Other Results (in Paper)
Victim Cells ≠ Weak Cells (i.e., leaky cells)
  Almost no overlap between them
Errors not strongly affected by temperature
  Default temperature: 50°C
  At 30°C and 70°C, number of errors changes <15%
Errors are repeatable
  Across ten iterations of testing, >70% of victim cells had errors in every iteration
Notes: First, we show that victim cells are not weak cells, which are cells that are inherently leaky. According to our experiments, we saw almost no overlap between them.
Second, we show that errors are not strongly affected by temperature. In all of the tests so far, we set the temperature to 50 degrees Celsius. But even when we changed the temperature by 20 degrees, the number of errors changed by less than 15 percent.
Third, we show that errors are repeatable. Across ten iterations of testing, more than 70% of victim cells had errors in every iteration.

## Slide 70: 6. Other Results (in Paper) cont’d
As many as 4 errors per cache-line
  Simple ECC (e.g., SECDED) cannot prevent all errors
Number of cells & rows affected by aggressor
  Victims cells per aggressor: ≤110
  Victims rows per aggressor: ≤9
Cells affected by two aggressors on either side
  Very small fraction of victim cells (<100) have an error when either one of the aggressors is toggled
Notes: Fourth, we show that there are as many as four errors per cacheline. From this, we conclude that simple ECC schemes (for example, SECDED) cannot prevent all errors.
Fifth, we show that the number of cells & rows affected by an aggressor can be as high as 110 or 9, respectively.
Lastly, we show that a very small fraction of victim cells experience an error when either one of the aggressors is toggled.

## Slide 71: More on RowHammer Analysis
Yoongu Kim, Ross Daly, Jeremie Kim, Chris Fallin, Ji Hye Lee, Donghyuk Lee, Chris Wilkerson, Konrad Lai, and Onur Mutlu, "Flipping Bits in Memory Without Accessing Them: An Experimental Study of DRAM Disturbance Errors" Proceedings of the 41st International Symposium on Computer Architecture (ISCA), Minneapolis, MN, June 2014. [Slides (pptx) (pdf)] [Lightning Session Slides (pptx) (pdf)] [Source Code and Data]

## Slide 72: Retrospective on RowHammer & Future
https://people.inf.ethz.ch/omutlu/pub/rowhammer-and-other-memory-issues_date17.pdf
Onur Mutlu, "The RowHammer Problem and Other Issues We May Face as Memory Becomes Denser" Invited Paper in Proceedings of the Design, Automation, and Test in Europe Conference (DATE), Lausanne, Switzerland, March 2017. [Slides (pptx) (pdf)]

## Slide 73: Challenge and Opportunity for Future
Fundamentally
Secure, Reliable, Safe
Computing Architectures

## Slide 74: Future Memory Reliability/Security Challenges

## Slide 75: Future of Main Memory
DRAM is becoming less reliable  more vulnerable

## Slide 76: Large-Scale Failure Analysis of DRAM Chips
Analysis and modeling of memory errors found in all of Facebook’s server fleet
Justin Meza, Qiang Wu, Sanjeev Kumar, and Onur Mutlu, "Revisiting Memory Errors in Large-Scale Production Data Centers: Analysis and Modeling of New Trends from the Field" Proceedings of the 45th Annual IEEE/IFIP International Conference on Dependable Systems and Networks (DSN), Rio de Janeiro, Brazil, June 2015. [Slides (pptx) (pdf)] [DRAM Error Model]

## Slide 77
Intuition: quadratic increase in capacity
DRAM Reliability Reducing
Meza+, “Revisiting Memory Errors in Large-Scale Production Data Centers,” DSN’15.

## Slide 78: Aside: SSD Error Analysis in the Field
First large-scale field study of flash memory errors
Justin Meza, Qiang Wu, Sanjeev Kumar, and Onur Mutlu, "A Large-Scale Study of Flash Memory Errors in the Field" Proceedings of the ACM International Conference on Measurement and Modeling of Computer Systems (SIGMETRICS), Portland, OR, June 2015. [Slides (pptx) (pdf)] [Coverage at ZDNet]

## Slide 79: Future of Main Memory
DRAM is becoming less reliable  more vulnerable
Due to difficulties in DRAM scaling, other problems may also appear (or they may be going unnoticed)
Some errors may already be slipping into the field
  Read disturb errors (Rowhammer)
  Retention errors
  Read errors, write errors
  …
These errors can also pose security vulnerabilities

## Slide 80: DRAM Data Retention Time Failures
Determining the data retention time of a cell/row is getting more difficult
Retention failures may already be slipping into the field

## Slide 81: Analysis of Data Retention Failures [ISCA’13]
Jamie Liu, Ben Jaiyen, Yoongu Kim, Chris Wilkerson, and Onur Mutlu, "An Experimental Study of Data Retention Behavior in Modern DRAM Devices: Implications for Retention Time Profiling Mechanisms" Proceedings of the 40th International Symposium on Computer Architecture (ISCA), Tel-Aviv, Israel, June 2013. Slides (ppt) Slides (pdf)

## Slide 82: Two Challenges to Retention Time Profiling
Data Pattern Dependence (DPD) of retention time
Variable Retention Time (VRT) phenomenon

## Slide 83: Two Challenges to Retention Time Profiling
Challenge 1: Data Pattern Dependence (DPD)
  Retention time of a DRAM cell depends on its value and the values of cells nearby it
  When a row is activated, all bitlines are perturbed simultaneously

## Slide 84: Data Pattern Dependence
Electrical noise on the bitline affects reliable sensing of a DRAM cell
The magnitude of this noise is affected by values of nearby cells via
  Bitline-bitline coupling  electrical coupling between adjacent bitlines
  Bitline-wordline coupling  electrical coupling between each bitline and the activated wordline
Notes: If a cell has lost enough charge, this noise can be large enough to cause a failure on a read
(normally, there is enough noise margin to tolerate the coupling noise)

## Slide 85: Data Pattern Dependence
Electrical noise on the bitline affects reliable sensing of a DRAM cell
The magnitude of this noise is affected by values of nearby cells via
  Bitline-bitline coupling  electrical coupling between adjacent bitlines
  Bitline-wordline coupling  electrical coupling between each bitline and the activated wordline
Retention time of a cell depends on data patterns stored in nearby cells
 need to find the worst data pattern to find worst-case retention time
 this pattern is location dependent
Notes: If a cell has lost enough charge, this noise can be large enough to cause a failure on a read
(normally, there is enough noise margin to tolerate the coupling noise)

## Slide 86: Two Challenges to Retention Time Profiling
Challenge 2: Variable Retention Time (VRT)
  Retention time of a DRAM cell changes randomly over time
    a cell alternates between multiple retention time states
  Leakage current of a cell changes sporadically due to a charge trap in the gate oxide of the DRAM cell access transistor
  When the trap becomes occupied, charge leaks more readily from the transistor’s drain, leading to a short retention time
    Called Trap-Assisted Gate-Induced Drain Leakage
  This process appears to be a random process [Kim+ IEEE TED’11]
  Worst-case retention time depends on a random process
     need to find the worst case despite this

## Slide 87: Modern DRAM Retention Time Distribution
Newer device families have more weak cells than older ones
Likely a result of technology scaling
OLDER
NEWER
OLDER
NEWER

## Slide 88: An Example VRT Cell
A cell from E 2Gb chip family

## Slide 89: Variable Retention Time
A 2Gb chip family
Min ret time = Max ret time
Expected if no VRT
Most failing cells
exhibit VRT
Many failing cells jump from
very high retention time to very low

## Slide 90: More on Data Retention Failures [ISCA’13]
Jamie Liu, Ben Jaiyen, Yoongu Kim, Chris Wilkerson, and Onur Mutlu, "An Experimental Study of Data Retention Behavior in Modern DRAM Devices: Implications for Retention Time Profiling Mechanisms" Proceedings of the 40th International Symposium on Computer Architecture (ISCA), Tel-Aviv, Israel, June 2013. Slides (ppt) Slides (pdf)

## Slide 91: Industry Is Writing Papers About It, Too

## Slide 92: Industry Is Writing Papers About It, Too

## Slide 93: Refresh Overhead: Performance
8%
46%
Liu et al., “RAIDR: Retention-Aware Intelligent DRAM Refresh,” ISCA 2012.

## Slide 94: Refresh Overhead: Energy
15%
47%
Liu et al., “RAIDR: Retention-Aware Intelligent DRAM Refresh,” ISCA 2012.

## Slide 95: Retention Time Profile of DRAM

## Slide 96: RAIDR: Eliminating Unnecessary Refreshes
Observation: Most DRAM rows can be refreshed much less often without losing data [Kim+, EDL’09][Liu+ ISCA’13]
Key idea: Refresh rows containing weak cells
more frequently, other rows less frequently
  1. Profiling: Profile retention time of all rows
  2. Binning: Store rows into bins by retention time in memory controller
  Efficient storage with Bloom Filters (only 1.25KB for 32GB memory)
  3. Refreshing: Memory controller refreshes rows in different bins at different rates
Results: 8-core, 32GB, SPEC, TPC-C, TPC-H
  74.6% refresh reduction @ 1.25KB storage
  ~16%/20% DRAM dynamic/idle power reduction
  ~9% performance improvement
  Benefits increase with DRAM capacity
Liu et al., “RAIDR: Retention-Aware Intelligent DRAM Refresh,” ISCA 2012.

## Slide 97: More on RAIDR: Perf+Energy Perspective
Jamie Liu, Ben Jaiyen, Richard Veras, and Onur Mutlu, "RAIDR: Retention-Aware Intelligent DRAM Refresh" Proceedings of the 39th International Symposium on Computer Architecture (ISCA), Portland, OR, June 2012. Slides (pdf)

## Slide 98: Finding DRAM Retention Failures
How can we reliably find the retention time of all DRAM cells?
Goals: so that we can
  Make DRAM reliable and secure
  Make techniques like RAIDR work
   improve performance and energy

## Slide 99: Mitigation of Retention Issues [SIGMETRICS’14]
Samira Khan, Donghyuk Lee, Yoongu Kim, Alaa Alameldeen, Chris Wilkerson, and Onur Mutlu, "The Efficacy of Error Mitigation Techniques for DRAM Retention Failures: A Comparative Experimental Study" Proceedings of the ACM International Conference on Measurement and Modeling of Computer Systems (SIGMETRICS), Austin, TX, June 2014. [Slides (pptx) (pdf)] [Poster (pptx) (pdf)] [Full data sets]

## Slide 100: Towards an Online Profiling System
Key Observations:
Testing alone cannot detect all possible failures
Combination of ECC and other mitigation techniques is much more effective
  But degrades performance
Testing can help to reduce the ECC strength
  Even when starting with a higher strength ECC
Khan+, “The Efficacy of Error Mitigation Techniques for DRAM Retention Failures: A Comparative Experimental Study,” SIGMETRICS 2014.
Notes: Our high-level design for online profiling system is based to thee key observations:

## Slide 101: Towards an Online Profiling System
Run tests periodically after a short interval
at smaller regions of memory
Initially Protect DRAM
with Strong ECC
1
Periodically Test
Parts of DRAM
2
ECC
Test
Test
Test
Mitigate errors and
reduce ECC
3
Notes: Based on these observations, we propose that in an online profiling system,

## Slide 102: Handling Variable Retention Time [DSN’15]
Moinuddin Qureshi, Dae Hyun Kim, Samira Khan, Prashant Nair, and Onur Mutlu, "AVATAR: A Variable-Retention-Time (VRT) Aware Refresh for DRAM Systems" Proceedings of the 45th Annual IEEE/IFIP International Conference on Dependable Systems and Networks (DSN), Rio de Janeiro, Brazil, June 2015. [Slides (pptx) (pdf)]

## Slide 103: AVATAR
Insight: Avoid retention failures  Upgrade row on ECC error
Observation: Rate of VRT >> Rate of soft error (50x-2500x)
A
B
C
D
E
F
G
H
DRAM Rows
RETENTION
PROFILING
Weak Cell
0
0
1
0
0
0
1
0
Ref. Rate Table
ECC
ECC
ECC
ECC
ECC
ECC
ECC
ECC
1
AVATAR mitigates VRT by increasing refresh rate on error
Scrub
(15 min)
Row protected from future
retention failures

## Slide 104: RESULTS: REFRESH SAVINGS
AVATAR
No VRT
AVATAR reduces refresh by 60%-70%, similar to multi rate refresh but with VRT tolerance
Retention Testing Once a Year can revert refresh saving from 60% to 70%

## Slide 105: SPEEDUP
Speedup
Chart: 
| 8Gb | 16Gb | 32Gb | 64Gb
AVATAR (1yr) | 1.04 | 1.065 | 1.13 | 1.35
NoRefresh | 1.05 | 1.09 | 1.21 | 1.54
AVATAR gets 2/3rd the performance of NoRefresh. More gains at higher capacity nodes

## Slide 106: ENERGY DELAY PRODUCT
Chart: 
| 8Gb | 16Gb | 32Gb | 64Gb
AVATAR (1yr) | 0.95 | 0.88 | 0.75 | 0.52
NoRefresh | 0.91 | 0.83 | 0.68 | 0.41
Energy Delay Product
AVATAR reduces EDP,
Significant reduction at higher capacity nodes

## Slide 107: Handling Data-Dependent Failures [DSN’16]
Samira Khan, Donghyuk Lee, and Onur Mutlu, "PARBOR: An Efficient System-Level Technique to Detect Data-Dependent Failures in DRAM" Proceedings of the 45th Annual IEEE/IFIP International Conference on Dependable Systems and Networks (DSN), Toulouse, France, June 2016. [Slides (pptx) (pdf)]

## Slide 108: Handling Data-Dependent Failures [MICRO’17]
Samira Khan, Chris Wilkerson, Zhe Wang, Alaa R. Alameldeen, Donghyuk Lee, and Onur Mutlu, "Detecting and Mitigating Data-Dependent DRAM Failures by Exploiting Current Memory Content" Proceedings of the 50th International Symposium on Microarchitecture (MICRO), Boston, MA, USA, October 2017. [Slides (pptx) (pdf)] [Lightning Session Slides (pptx) (pdf)] [Poster (pptx) (pdf)]

## Slide 109: Handling Both DPD and VRT [ISCA’17]
Minesh Patel, Jeremie S. Kim, and Onur Mutlu, "The Reach Profiler (REAPER): Enabling the Mitigation of DRAM Retention Failures via Profiling at Aggressive Conditions" Proceedings of the 44th International Symposium on Computer Architecture (ISCA), Toronto, Canada, June 2017. [Slides (pptx) (pdf)] [Lightning Session Slides (pptx) (pdf)]
First experimental analysis of (mobile) LPDDR4 chips
Analyzes the complex tradeoff space of retention time profiling
Idea: enable fast and robust profiling at higher refresh intervals & temperatures

## Slide 110: The Reach Profiler (REAPER): Enabling the Mitigation of DRAM Retention Failures via Profiling at Aggressive Conditions
Minesh Patel Jeremie S. Kim
Onur Mutlu
Notes: Hi, I’m Minesh Patel from ETH Zurich
and today, I’ll talk about the reach profiler, a new methodology for DRAM retention failure profiling

## Slide 111
SA
SA
SA
SA
SA
Row Decoder
DRAM
Leaky
Notes: DRAM is composed of a heterogeneous set of cells with various different leakage rates

## Slide 112
Leaky Cells
Periodic DRAM Refresh
Performance + Energy Overhead
Notes: This requires a process called DRAM refresh in order to periodically restore charge to the leaky cells
However, this results in significant system performance and energy penalties.

## Slide 113
Goal: find all retention failures for
a refresh interval T > default (64ms)
SA
SA
SA
SA
SA
Row Decoder
Notes: Ideally, we would like to identify all the cells that fail at a given refresh interval so that we can extend the default refresh interval past 64ms and mitigate DRAM refresh overhead

## Slide 114
Variable retention time
Data pattern dependence
Process, voltage, temperature
Notes: However, there are a number of unwanted effects that complicate profiling, which I will go into in detail in my talk later this afternoon

## Slide 115
Characterization of
368 LPDDR4 DRAM Chips
1
2
Cells are more likely to fail at an
increased (refresh interval | temperature)
Complex tradeoff space between profiling
(speed & coverage & false positives)
Notes: In order to better understand these effects in modern DRAM, we perform the first extensive characterization of 368 LPDDR4 DRAM chips
We make two major observations
First, we find that cells are more likely to fail at an increased refresh interval or temperature
Second, we identify a complex tradeoff space surrounding profiling, and characterize it in terms of profiling speed, failure coverage, and false positive rate

## Slide 116
refresh interval
temperature
operate
here
Notes: We leverage these observations to develop the reach profiler, which searches for failures NOT at the operating conditions,

## Slide 117
refresh interval
temperature
REACH
PROFILING
profile
here
operate
here
Notes: But rather at reach conditions, where cells are more likely to fail

## Slide 118
+ Faster and more reliable
than current approaches
Reach Profiling
A new DRAM retention failure profiling methodology
+ Enables longer refresh intervals
Notes: We find that this not only increases profiling speed and reliability beyond prior approaches to profiling,
But also enables longer refresh intervals that were previously unreasonable due to profiling overhead

## Slide 119: Handling Both DPD and VRT [ISCA’17]
Minesh Patel, Jeremie S. Kim, and Onur Mutlu, "The Reach Profiler (REAPER): Enabling the Mitigation of DRAM Retention Failures via Profiling at Aggressive Conditions" Proceedings of the 44th International Symposium on Computer Architecture (ISCA), Toronto, Canada, June 2017. [Slides (pptx) (pdf)] [Lightning Session Slides (pptx) (pdf)]
First experimental analysis of (mobile) LPDDR4 chips
Analyzes the complex tradeoff space of retention time profiling
Idea: enable fast and robust profiling at higher refresh intervals & temperatures

## Slide 120: The DRAM Latency PUF: Quickly Evaluating Physical Unclonable Functions by Exploiting the Latency-Reliability Tradeoff in Modern Commodity DRAM Devices
Jeremie S. Kim Minesh Patel
Hasan Hassan Onur Mutlu
QR Code for the paper
https://people.inf.ethz.ch/omutlu/pub/dram-latency-puf_hpca18.pdf
HPCA 2018
Notes: Please come to my talk at HPCA 2018, if you would like to learn more or have any questions. Thank you very much.

## Slide 121: How Do We Keep Memory Secure?
DRAM
Flash memory
Emerging Technologies
  Phase Change Memory
  STT-MRAM
  RRAM, memristors
  …

## Slide 122: Solution Direction: Principled Designs
Design fundamentally secure
computing architectures
Predict and prevent
such safety issues

## Slide 123: How Do We Keep Memory Secure?
Understand: Solid methodologies for failure modeling and discovery
  Modeling based on real device data – small scale and large scale
  Metrics for secure architectures
Architect: Principled co-architecting of system and memory
  Good partitioning of duties across the stack
  Patch-ability in the field
Design & Test: Principled electronic design, automation, testing
  Design for security
  High coverage and good interaction with reliability methods

## Slide 124
  Kim+, “Flipping Bits in Memory Without Accessing Them: An Experimental Study of DRAM Disturbance Errors,” ISCA 2014.
Temperature
Controller
PC
Heater
FPGAs
FPGAs
Understand and Model with Experiments (DRAM)

## Slide 125: Understand and Model with Experiments (Flash)
USB Jack
Virtex-II Pro
(USB controller)
Virtex-V FPGA
(NAND Controller)
HAPS-52 Mother Board
USB Daughter Board
NAND Daughter Board
1x-nm
NAND Flash
[DATE 2012, ICCD 2012, DATE 2013, ITJ 2013, ICCD 2013, SIGMETRICS 2014, HPCA 2015, DSN 2015, MSST 2015, JSAC 2016, HPCA 2017, DFRWS 2017,
PIEEE’17, HPCA’18]
Cai+, “Error Characterization, Mitigation, and Recovery in Flash Memory Based Solid State Drives,” Proc. IEEE 2017.

## Slide 126: Understanding Flash Memory Reliability
https://arxiv.org/pdf/1706.08642
Proceedings of the IEEE, Sept. 2017

## Slide 127: Understanding Flash Memory Reliability
Justin Meza, Qiang Wu, Sanjeev Kumar, and Onur Mutlu, "A Large-Scale Study of Flash Memory Errors in the Field" Proceedings of the ACM International Conference on Measurement and Modeling of Computer Systems (SIGMETRICS), Portland, OR, June 2015. [Slides (pptx) (pdf)] [Coverage at ZDNet] [Coverage on The Register] [Coverage on TechSpot] [Coverage on The Tech Report]

## Slide 128: NAND Flash Vulnerabilities [HPCA’17]
https://people.inf.ethz.ch/omutlu/pub/flash-memory-programming-vulnerabilities_hpca17.pdf
HPCA, Feb. 2017

## Slide 129: 3D NAND Flash Reliability I [HPCA’18]
Yixin Luo, Saugata Ghose, Yu Cai, Erich F. Haratsch, and Onur Mutlu, "HeatWatch: Improving 3D NAND Flash Memory Device Reliability by Exploiting Self-Recovery and Temperature-Awareness" Proceedings of the 24th International Symposium on High-Performance Computer Architecture (HPCA), Vienna, Austria, February 2018. [Lightning Talk Video] [Slides (pptx) (pdf)] [Lightning Session Slides (pptx) (pdf)]

## Slide 130: 3D NAND Flash Reliability II [SIGMETRICS’18]
Yixin Luo, Saugata Ghose, Yu Cai, Erich F. Haratsch, and Onur Mutlu, "Improving 3D NAND Flash Memory Lifetime by Tolerating Early Retention Loss and Process Variation" Proceedings of the ACM International Conference on Measurement and Modeling of Computer Systems (SIGMETRICS), Irvine, CA, USA, June 2018. [Abstract]

## Slide 131: If Time Permits: NAND Flash Vulnerabilities
Yu Cai, Saugata Ghose, Erich F. Haratsch, Yixin Luo, and Onur Mutlu, "Error Characterization, Mitigation, and Recovery in Flash Memory Based Solid State Drives" to appear in Proceedings of the IEEE, 2017.
Cai+, “Error Patterns in MLC NAND Flash Memory: Measurement, Characterization, and Analysis,” DATE 2012.
Cai+, “Flash Correct-and-Refresh: Retention-Aware Error Management for Increased Flash Memory Lifetime,” ICCD 2012.
Cai+, “Threshold Voltage Distribution in MLC NAND Flash Memory: Characterization, Analysis and Modeling,” DATE 2013.
Cai+, “Error Analysis and Retention-Aware Error Management for NAND Flash Memory,” Intel Technology Journal 2013.
Cai+, “Program Interference in MLC NAND Flash Memory: Characterization, Modeling, and Mitigation,” ICCD 2013.
Cai+, “Neighbor-Cell Assisted Error Correction for MLC NAND Flash Memories,” SIGMETRICS 2014.
Cai+,”Data Retention in MLC NAND Flash Memory: Characterization, Optimization and Recovery,” HPCA 2015.
Cai+, “Read Disturb Errors in MLC NAND Flash Memory: Characterization and Mitigation,” DSN 2015.
Luo+, “WARM: Improving NAND Flash Memory Lifetime with Write-hotness Aware Retention Management,” MSST 2015.
Meza+, “A Large-Scale Study of Flash Memory Errors in the Field,” SIGMETRICS 2015.
Luo+, “Enabling Accurate and Practical Online Flash Channel Modeling for Modern MLC NAND Flash Memory,” IEEE JSAC 2016.
Cai+, “Vulnerabilities in MLC NAND Flash Memory Programming: Experimental Analysis, Exploits, and Mitigation Techniques,” HPCA 2017.
Fukami+, “Improving the Reliability of Chip-Off Forensic Analysis of NAND Flash Memory Devices,” DFRWS EU 2017.
Cai+, “Error Characterization, Mitigation, and Recovery in Flash Memory Based Solid State Drives,” Proc. IEEE 2017.

## Slide 132: There are Two Other Solution Directions
New Technologies: Replace or (more likely) augment DRAM with a different technology
  Non-volatile memories
Embracing Un-reliability:
Design memories with different reliability
and store data intelligently across them
[Luo+ DSN 2014]
…
Fundamental solutions to security require co-design across the hierarchy
Micro-architecture
SW/HW Interface
Program/Language
Algorithm
Problem
Logic
Devices
System Software
Electrons

## Slide 133: Exploiting Memory Error Tolerance with Hybrid Memory Systems
Chart: Memory error vulnerability
| App/Data A | App/Data B | App/Data C
System/Application Crash | 1.0414 | 0.63898 | 0.24773
Vulnerable data
Tolerant data
Heterogeneous-Reliability Memory [DSN 2014]
Low-cost memory
Reliable memory
Vulnerable data
Tolerant data
Vulnerable data
Tolerant data
ECC protected
Well-tested chips
NoECC or Parity
Less-tested chips
  On Microsoft’s Web Search workload
  Reduces server hardware cost by 4.7 %
  Achieves single server availability target of 99.90 %
Notes: As we have shown earlier, either across or within applications, our characterization can identify data that are vulnerable to memory errors and data that are tolerant to memory errors.
To exploit this observation, we would like to map these different data onto different memory modules according to their memory error tolerance.
As an example here, we map vulnerable data to reliable memory to improve reliability, and map tolerant data to low-cost less-reliable memory to exploit its tolerance and lower the cost. We call this mechanism heterogeneous-reliability memory, HRM.
Reliable memory consists of … Low cost memory consists of …
As we will show later, HRM allows us to use weaker error protection in memory, and enables the use of less-tested memory chips to lower the cost of the memory system, while still achieving reasonable single-server reliability target.

## Slide 134: More on Heterogeneous-Reliability Memory
Yixin Luo, Sriram Govindan, Bikash Sharma, Mark Santaniello, Justin Meza, Aman Kansal, Jie Liu, Badriddine Khessib, Kushagra Vaid, and Onur Mutlu, "Characterizing Application Memory Error Vulnerability to Optimize Data Center Cost via Heterogeneous-Reliability Memory" Proceedings of the 44th Annual IEEE/IFIP International Conference on Dependable Systems and Networks (DSN), Atlanta, GA, June 2014. [Summary] [Slides (pptx) (pdf)] [Coverage on ZDNet]

## Slide 135: Summary: Memory Reliability and Security
Memory reliability is reducing
Reliability issues open up security vulnerabilities
  Very hard to defend against
Rowhammer is an example
  Its implications on system security research are tremendous & exciting
Good news: We have a lot more to do.
Understand: Solid methodologies for failure modeling and discovery
  Modeling based on real device data – small scale and large scale
Architect: Principled co-architecting of system and memory
  Good partitioning of duties across the stack
Design & Test: Principled electronic design, automation, testing
  High coverage and good interaction with system reliability methods

## Slide 136: Challenge and Opportunity for Future
Fundamentally
Secure, Reliable, Safe
Computing Architectures

## Slide 137: One Important Takeaway
Main Memory Needs
Intelligent Controllers

## Slide 138: Flash Memory Reliability and Security

## Slide 139: Evolution of NAND Flash Memory
Flash memory is widening its range of applications
  Portable consumer devices, laptop PCs and enterprise servers
Seaung Suk Lee, “Emerging Challenges in NAND Flash Technology”, Flash Summit 2011 (Hynix)
CMOS scaling
More bits per Cell

## Slide 140: Flash Challenges: Reliability and Endurance
E. Grochowski et al., “Future technology challenges for NAND flash and HDD products”, Flash Memory Summit 2012
P/E cycles (required)
P/E cycles (provided)
A few thousand
Writing
the full capacity
of the drive
10 times per day
for 5 years
(STEC)
> 50k P/E cycles

## Slide 141: NAND Flash Memory is Increasingly Noisy
Noisy NAND
Write
Read

## Slide 142: Future NAND Flash-based Storage Architecture
Memory
Signal
Processing
Error
Correction
Raw Bit
Error Rate
Uncorrectable
BER < 10-15
Noisy
High
Lower
Build reliable error models for NAND flash memory
Design efficient reliability mechanisms based on the model
Our Goals:
Better

## Slide 143: NAND Flash Error Model
Noisy NAND
Write
Read
Experimentally characterize and model dominant errors
Neighbor page prog/read (c-to-c interference)
Retention
Erase block
Program page
Write
Read
Cai et al., “Threshold voltage distribution in MLC NAND Flash Memory: Characterization, Analysis, and Modeling”, DATE 2013
Cai et al., “Vulnerabilities in MLC NAND Flash Memory Programming: Experimental Analysis, Exploits, and Mitigation Techniques”, HPCA 2017
Cai et al., “Flash Correct-and-Refresh: Retention-aware error management for increased flash memory lifetime”, ICCD 2012
Cai et al., “Program Interference in MLC NAND Flash Memory: Characterization, Modeling, and Mitigation”, ICCD 2013
Cai et al., “Neighbor-Cell Assisted Error Correction in MLC NAND Flash Memories”, SIGMETRICS 2014
Cai et al., “Read Disturb Errors in MLC NAND Flash Memory: Characterization and Mitigation”, DSN 2015
Cai et al., “Error Patterns in MLC NAND Flash Memory: Measurement, Characterization, and Analysis””, DATE 2012
Cai et al., “Error Analysis and Retention-Aware Error Management for NAND Flash Memory”, ITJ 2013
Cai et al., “Data Retention in MLC NAND Flash Memory: Characterization, Optimization and Recovery”, HPCA 2015
Luo et al., “Enabling Accurate and Practical Online Flash Channel Modeling for Modern MLC NAND Flash Memory”, JSAC 2016

## Slide 144: Our Goals and Approach
Goals:
  Understand error mechanisms and develop reliable predictive models for MLC NAND flash memory errors
  Develop efficient error management techniques to mitigate errors and improve flash reliability and endurance
Approach:
  Solid experimental analyses of errors in real MLC NAND flash memory  drive the understanding and models
  Understanding, models, and creativity  drive the new techniques

## Slide 145: Experimental Testing Platform
USB Jack
Virtex-II Pro
(USB controller)
Virtex-V FPGA
(NAND Controller)
HAPS-52 Mother Board
USB Daughter Board
NAND Daughter Board
1x-nm
NAND Flash
[DATE 2012, ICCD 2012, DATE 2013, ITJ 2013, ICCD 2013, SIGMETRICS 2014, HPCA 2015, DSN 2015, MSST 2015, JSAC 2016, HPCA 2017, DFRWS 2017,
PIEEE’17, HPCA’18]
Cai+, “Error Characterization, Mitigation, and Recovery in Flash Memory Based Solid State Drives,” Proc. IEEE 2017.

## Slide 146: NAND Flash Error Types
Four types of errors [Cai+, DATE 2012]
Caused by common flash operations
  Read errors
  Erase errors
  Program (interference) errors
Caused by flash cell losing charge over time
  Retention errors
    Whether an error happens depends on required retention time
    Especially problematic in MLC flash because threshold voltage window to determine stored value is smaller

## Slide 147: Observations: Flash Error Analysis
retention errors
Raw bit error rate increases exponentially with P/E cycles
Retention errors are dominant (>99% for 1-year ret. time)
Retention errors increase with retention time requirement
P/E Cycles
Raw Bit Error Rate
Cai et al., Error Patterns in MLC NAND Flash Memory, DATE 2012.

## Slide 148: More on Flash Error Analysis
Yu Cai, Erich F. Haratsch, Onur Mutlu, and Ken Mai, "Error Patterns in MLC NAND Flash Memory: Measurement, Characterization, and Analysis" Proceedings of the Design, Automation, and Test in Europe Conference (DATE), Dresden, Germany, March 2012. Slides (ppt)

## Slide 149: Solution to Retention Errors
Refresh periodically
Change the period based on P/E cycle wearout
  Refresh more often at higher P/E cycles
Use a combination of in-place and remapping-based refresh
Cai et al. “Flash Correct-and-Refresh: Retention-Aware Error Management for Increased Flash Memory Lifetime”, ICCD 2012.

## Slide 150: Flash Correct-and-Refresh [ICCD’12]
Yu Cai, Gulay Yalcin, Onur Mutlu, Erich F. Haratsch, Adrian Cristal, Osman Unsal, and Ken Mai, "Flash Correct-and-Refresh: Retention-Aware Error Management for Increased Flash Memory Lifetime" Proceedings of the 30th IEEE International Conference on Computer Design (ICCD), Montreal, Quebec, Canada, September 2012. Slides (ppt)(pdf)

## Slide 151: Many Errors and Their Mitigation [PIEEE’17]
Cai+, “Error Characterization, Mitigation, and Recovery in Flash Memory Based Solid State Drives,” Proc. IEEE 2017.

## Slide 152: Many Errors and Their Mitigation [PIEEE’17]
https://arxiv.org/pdf/1706.08642
Proceedings of the IEEE, Sept. 2017

## Slide 153: One Issue: Read Disturb in Flash Memory
All scaled memories are prone to read disturb errors
DRAM
SRAM
Hard Disks: Adjacent Track Interference
NAND Flash

## Slide 154: NAND Flash Memory Background
Flash Memory
Page 1
Page 0
Page 2
Page 255
……
Page 257
Page 256
Page 258
Page 511
……
……
Page M+1
Page M
Page M+2
Page M+255
……
Flash Controller
Block 0
Block 1
Block N
Read
Pass
Pass
…
Pass
Notes: When we read from one page in a block, we apply a high voltage to all the other pages in the same block. We will explain why later

## Slide 155: Flash Cell Array
Sense Amplifiers
Block X
Page Y
Sense Amplifiers
Row
Column
Notes: Now, let’s zoom in to a single block of flash memory, which consists of an array of flash pages.
Each flash page is written to flash cells located in the same row.
Each row of cells are controlled by the same horizontal wire.
Each column of cells are connected in series with a sense amplifier at the bottom.

## Slide 156: Flash Cell
Floating Gate
Gate
Drain
Source
Floating Gate Transistor
(Flash Cell)
Vth = 2.5 V
Notes: Now let’s zoom in again to look at a single flash cell, or, it can also be called, a floating gate transistor.

## Slide 157: Flash Read
Vread = 2.5 V
Vth = 3 V
Vth = 2 V
1
0
Vread = 2.5 V
Gate
Notes: Now, if we have two flash cells programmed to different threshold voltages, 2V and 3V, we can distinguish them with a read voltage of 2.5V.
When we apply 2.5V to the gate, since the read voltage is higher than the threshold voltage, …
Now if we look back at this example, we can see that the threshold voltage of each flash cell actually represents the value being stored.

## Slide 158: Flash Pass-Through
Vpass = 5 V
Vth = 2 V
1
Vpass = 5 V
Gate
1
Vth = 3 V
Notes: But, for the same cells, when we apply a high voltage to them, regardless of the threshold voltage, any cell will be passed-through.
So we call this voltage pass-through voltage or Vpass

## Slide 159: Read from Flash Cell Array
3.0V
3.8V
3.9V
4.8V
3.5V
2.9V
2.4V
2.1V
2.2V
4.3V
4.6V
1.8V
3.5V
2.3V
1.9V
4.3V
Vread = 2.5 V
Vpass = 5.0 V
Vpass = 5.0 V
Vpass = 5.0 V
1
1
0
0
Correct values for page 2:
Page 1
Page 2
Page 3
Page 4
Pass (5V)
Read (2.5V)
Pass (5V)
Pass (5V)
Notes: Now, let’s look at an example array of flash cells.
In this example, we make up threshold voltage numbers for each cell.
Let’s say we want to read from the second page in this array.
So we apply a read voltage of 2.5 V to the second page
And since all the other pages are connected in series, we apply a high pass-through voltage of 5 V to the other pages.
As we can see, the high pass through voltage switches on all the flash pages being passed-through, allowing the sense amplifier to read the values stored in the second page.
In this case, the correct values …

## Slide 160: Read Disturb Problem: “Weak Programming” Effect
3.0V
3.8V
3.9V
4.8V
3.5V
2.9V
2.4V
2.1V
2.2V
4.3V
4.6V
1.8V
3.5V
2.3V
1.9V
4.3V
Repeatedly read page 3 (or any page other than page 2)
Read (2.5V)
Pass (5V)
Pass (5V)
Pass (5V)
Page 1
Page 2
Page 3
Page 4
Notes: However, the high pass through voltage can generate read disturb problem, which we will introduce now.
When we want to read page 3, instead of page 2, this high pass through voltage now needs to be applied on the 2nd page.
When we repeatedly read page 3, the pass through voltage induces a weak programming effect on the second page.

## Slide 161: Read Disturb Problem: “Weak Programming” Effect
Vread = 2.5 V
Vpass = 5.0 V
Vpass = 5.0 V
Vpass = 5.0 V
0
1
0
0
High pass-through voltage induces “weak-programming” effect
3.0V
3.8V
3.9V
4.8V
3.5V
2.9V
2.1V
2.2V
4.3V
4.6V
1.8V
3.5V
2.3V
1.9V
4.3V
Incorrect values from page 2:
2.4V
2.6V
Page 1
Page 2
Page 3
Page 4
Notes: As the weak programming effect accumulates, the threshold voltage of each flash cell increases, and the threshold voltage state of a cell can be altered.
In this case, when we read page 2 again, we will read incorrect values from page 2, 0001
Flash vendors conservatively set this pass-through voltage to a high voltage.
However, we find in the paper that it is unnecessary to set to this high, and that reducing this voltage by just a bit will reduce read disturb errors significantly in the future.

## Slide 162: Executive Summary [DSN’15]
Read disturb errors limit flash memory lifetime today
  Apply a high pass-through voltage (Vpass) to multiple pages on a read
  Repeated application of Vpass can alter stored values in unread pages
We characterize read disturb on real NAND flash chips
  Slightly lowering Vpass greatly reduces read disturb errors
  Some flash cells are more prone to read disturb
Technique 1: Mitigate read disturb errors online
  Vpass Tuning dynamically finds and applies a lowered Vpass per block
  Flash memory lifetime improves by 21%
Technique 2: Recover after failure to prevent data loss
  Read Disturb Oriented Error Recovery (RDR) selectively corrects cells more susceptible to read disturb errors
  Reduces raw bit error rate (RBER) by up to 36%
Notes: When we read data from one page, we have to apply a high voltage to multiple other flash pages that are connected to this page, and we call this high pass-through voltage.
Over time this high pass-through voltage can alter the values stored in unread flash pages. We call this a read disturb error.
For the first time in open literature, we characterize read disturb on real NAND flash chips, and show that read disturb errors exist in today’s flash chips and is expected to increase in the future.
We make two key observations from the characterization.
Using our characterization, we develop two techniques that can help flash memory tolerate such read disturb errors.

## Slide 163: Read Disturb Prone vs. Resistant Cells
R
P
Disturb-Resistant
Disturb-Prone
Normalized Vth
PDF
N read disturbs
N read disturbs
R
P
Notes: RDR exploits each cell’s read disturb resistance.
Because of process variation, each cell can be classified as either disturb resistant or disturb prone.
After the same amount of read disturbs, the threshold voltage of a disturb-resistant cell does not change much, but the threshold voltage change of a disturb-prone cell is high.

## Slide 164: Observation 2: Some Flash Cells Are More Prone to Read Disturb
P1
ER
Normalized Vth
PDF
P
P
P
P
R
P
R
P
R
P
R
P
Disturb-prone cells have higher threshold voltages
Disturb-resistant cells have lower threshold voltages
After 250K read disturbs:
Disturb-prone ER state
Disturb-resistant P1 state
Notes: As our fourth observation, we find some flash cells are more prone to read disturb.
Now lets look at an example of the erased and P1 state.
With no read disturb, the threshold voltage of disturb prone and resistant cells are randomly distributed.
After a significant amount of read disturb, the cells redistribute because of read disturb.
At this point, we can see that disturb-prone cells have higher threshold voltages within each state,
And disturb-resistant cells have lower threshold voltages.
Now, if we look at the cells susceptible to errors, which are cells with threshold voltage closer to the boundary.
The disturb-prone cells are from the erased state, and the disturb-resistant cells are from the P1 state.

## Slide 165: Read Disturb Oriented Error Recovery (RDR)
Triggered by an uncorrectable flash error
  Back up all valid data in the faulty block
  Disturb the faulty page 100K times (more)
  Compare Vth’s before and after read disturb
  Select cells susceptible to flash errors (Vref−σ<Vth<Vref−σ)
  Predict among these susceptible cells
    Cells with more Vth shifts are disturb-prone  Higher Vth state
    Cells with less Vth shifts are disturb-resistant  Lower Vth state
Reduces total error count by up to 36% @ 1M read disturbs
ECC can be used to correct the remaining errors
Notes: Based on this finding, we propose read disturb oriented error recovery to identify disturb-prone and resistant cells after a failure has happened to recover from read disturb errors.
After an uncorrectable flash error, the following steps are triggered.

## Slide 166: More on Flash Read Disturb Errors [DSN’15]
Yu Cai, Yixin Luo, Saugata Ghose, Erich F. Haratsch, Ken Mai, and Onur Mutlu, "Read Disturb Errors in MLC NAND Flash Memory: Characterization and Mitigation" Proceedings of the 45th Annual IEEE/IFIP International Conference on Dependable Systems and Networks (DSN), Rio de Janeiro, Brazil, June 2015.

## Slide 167: Large-Scale SSD Error Analysis [SIGMETRICS’15]
First large-scale field study of flash memory errors
Justin Meza, Qiang Wu, Sanjeev Kumar, and Onur Mutlu, "A Large-Scale Study of Flash Memory Errors in the Field" Proceedings of the ACM International Conference on Measurement and Modeling of Computer Systems (SIGMETRICS), Portland, OR, June 2015. [Slides (pptx) (pdf)] [Coverage at ZDNet] [Coverage on The Register] [Coverage on TechSpot] [Coverage on The Tech Report]

## Slide 168: Another Lecture: NAND Flash Reliability
Yu Cai, Saugata Ghose, Erich F. Haratsch, Yixin Luo, and Onur Mutlu, "Error Characterization, Mitigation, and Recovery in Flash Memory Based Solid State Drives" to appear in Proceedings of the IEEE, 2017.
Cai+, “Error Patterns in MLC NAND Flash Memory: Measurement, Characterization, and Analysis,” DATE 2012.
Cai+, “Flash Correct-and-Refresh: Retention-Aware Error Management for Increased Flash Memory Lifetime,” ICCD 2012.
Cai+, “Threshold Voltage Distribution in MLC NAND Flash Memory: Characterization, Analysis and Modeling,” DATE 2013.
Cai+, “Error Analysis and Retention-Aware Error Management for NAND Flash Memory,” Intel Technology Journal 2013.
Cai+, “Program Interference in MLC NAND Flash Memory: Characterization, Modeling, and Mitigation,” ICCD 2013.
Cai+, “Neighbor-Cell Assisted Error Correction for MLC NAND Flash Memories,” SIGMETRICS 2014.
Cai+,”Data Retention in MLC NAND Flash Memory: Characterization, Optimization and Recovery,” HPCA 2015.
Cai+, “Read Disturb Errors in MLC NAND Flash Memory: Characterization and Mitigation,” DSN 2015.
Luo+, “WARM: Improving NAND Flash Memory Lifetime with Write-hotness Aware Retention Management,” MSST 2015.
Meza+, “A Large-Scale Study of Flash Memory Errors in the Field,” SIGMETRICS 2015.
Luo+, “Enabling Accurate and Practical Online Flash Channel Modeling for Modern MLC NAND Flash Memory,” IEEE JSAC 2016.
Cai+, “Vulnerabilities in MLC NAND Flash Memory Programming: Experimental Analysis, Exploits, and Mitigation Techniques,” HPCA 2017.
Fukami+, “Improving the Reliability of Chip-Off Forensic Analysis of NAND Flash Memory Devices,” DFRWS EU 2017.
Cai+, “Error Characterization, Mitigation, and Recovery in Flash Memory Based Solid State Drives,” Proc. IEEE 2017.

## Slide 169: NAND Flash Vulnerabilities [HPCA’17]
https://people.inf.ethz.ch/omutlu/pub/flash-memory-programming-vulnerabilities_hpca17.pdf
HPCA, Feb. 2017

## Slide 170: NAND Flash Errors: A Modern Survey
https://arxiv.org/pdf/1706.08642
Proceedings of the IEEE, Sept. 2017

## Slide 171: Summary: Memory Reliability and Security
Memory reliability is reducing
Reliability issues open up security vulnerabilities
  Very hard to defend against
Rowhammer is an example
  Its implications on system security research are tremendous & exciting
Good news: We have a lot more to do.
Understand: Solid methodologies for failure modeling and discovery
  Modeling based on real device data – small scale and large scale
Architect: Principled co-architecting of system and memory
  Good partitioning of duties across the stack
Design & Test: Principled electronic design, automation, testing
  High coverage and good interaction with system reliability methods

## Slide 172: Other Works on Flash Memory

## Slide 173: NAND Flash Error Model
Noisy NAND
Write
Read
Experimentally characterize and model dominant errors
Neighbor page prog/read (c-to-c interference)
Retention
Erase block
Program page
Write
Read
Cai et al., “Threshold voltage distribution in MLC NAND Flash Memory: Characterization, Analysis, and Modeling”, DATE 2013
Cai et al., “Vulnerabilities in MLC NAND Flash Memory Programming: Experimental Analysis, Exploits, and Mitigation Techniques”, HPCA 2017
Cai et al., “Flash Correct-and-Refresh: Retention-aware error management for increased flash memory lifetime”, ICCD 2012
Cai et al., “Program Interference in MLC NAND Flash Memory: Characterization, Modeling, and Mitigation”, ICCD 2013
Cai et al., “Neighbor-Cell Assisted Error Correction in MLC NAND Flash Memories”, SIGMETRICS 2014
Cai et al., “Read Disturb Errors in MLC NAND Flash Memory: Characterization and Mitigation”, DSN 2015
Cai et al., “Error Patterns in MLC NAND Flash Memory: Measurement, Characterization, and Analysis””, DATE 2012
Cai et al., “Error Analysis and Retention-Aware Error Management for NAND Flash Memory, ITJ 2013
Cai et al., “Data Retention in MLC NAND Flash Memory: Characterization, Optimization and Recovery" , HPCA 2015
Luo et al., “Enabling Accurate and Practical Online Flash Channel Modeling for Modern MLC NAND Flash Memory”, JSAC 2016

## Slide 174: Threshold Voltage Distribution
Yu Cai, Erich F. Haratsch, Onur Mutlu, and Ken Mai, "Threshold Voltage Distribution in MLC NAND Flash Memory: Characterization, Analysis and Modeling" Proceedings of the Design, Automation, and Test in Europe Conference (DATE), Grenoble, France, March 2013. Slides (ppt)

## Slide 175: Program Interference and Vref Prediction
Yu Cai, Onur Mutlu, Erich F. Haratsch, and Ken Mai, "Program Interference in MLC NAND Flash Memory: Characterization, Modeling, and Mitigation" Proceedings of the 31st IEEE International Conference on Computer Design (ICCD), Asheville, NC, October 2013. Slides (pptx) (pdf) Lightning Session Slides (pdf)

## Slide 176: Neighbor-Assisted Error Correction
Yu Cai, Gulay Yalcin, Onur Mutlu, Eric Haratsch, Osman Unsal, Adrian Cristal, and Ken Mai, "Neighbor-Cell Assisted Error Correction for MLC NAND Flash Memories" Proceedings of the ACM International Conference on Measurement and Modeling of Computer Systems (SIGMETRICS), Austin, TX, June 2014. Slides (ppt) (pdf)

## Slide 177: Data Retention
Yu Cai, Yixin Luo, Erich F. Haratsch, Ken Mai, and Onur Mutlu, "Data Retention in MLC NAND Flash Memory: Characterization, Optimization and Recovery" Proceedings of the 21st International Symposium on High-Performance Computer Architecture (HPCA), Bay Area, CA, February 2015. [Slides (pptx) (pdf)]

## Slide 178: SSD Error Analysis in the Field
First large-scale field study of flash memory errors
Justin Meza, Qiang Wu, Sanjeev Kumar, and Onur Mutlu, "A Large-Scale Study of Flash Memory Errors in the Field" Proceedings of the ACM International Conference on Measurement and Modeling of Computer Systems (SIGMETRICS), Portland, OR, June 2015. [Slides (pptx) (pdf)] [Coverage at ZDNet] [Coverage on The Register] [Coverage on TechSpot] [Coverage on The Tech Report]

## Slide 179: Flash Memory Programming Vulnerabilities
Yu Cai, Saugata Ghose, Yixin Luo, Ken Mai, Onur Mutlu, and Erich F. Haratsch, "Vulnerabilities in MLC NAND Flash Memory Programming: Experimental Analysis, Exploits, and Mitigation Techniques" Proceedings of the 23rd International Symposium on High-Performance Computer Architecture (HPCA) Industrial Session, Austin, TX, USA, February 2017. [Slides (pptx) (pdf)] [Lightning Session Slides (pptx) (pdf)]

## Slide 180: Accurate and Online Channel Modeling
Yixin Luo, Saugata Ghose, Yu Cai, Erich F. Haratsch, and Onur Mutlu, "Enabling Accurate and Practical Online Flash Channel Modeling for Modern MLC NAND Flash Memory" to appear in IEEE Journal on Selected Areas in Communications (JSAC), 2016.

## Slide 181: 3D NAND Flash Reliability I [HPCA’18]
Yixin Luo, Saugata Ghose, Yu Cai, Erich F. Haratsch, and Onur Mutlu, "HeatWatch: Improving 3D NAND Flash Memory Device Reliability by Exploiting Self-Recovery and Temperature-Awareness" Proceedings of the 24th International Symposium on High-Performance Computer Architecture (HPCA), Vienna, Austria, February 2018. [Lightning Talk Video] [Slides (pptx) (pdf)] [Lightning Session Slides (pptx) (pdf)]

## Slide 182: 3D NAND Flash Reliability II [SIGMETRICS’18]
Yixin Luo, Saugata Ghose, Yu Cai, Erich F. Haratsch, and Onur Mutlu, "Improving 3D NAND Flash Memory Lifetime by Tolerating Early Retention Loss and Process Variation" Proceedings of the ACM International Conference on Measurement and Modeling of Computer Systems (SIGMETRICS), Irvine, CA, USA, June 2018. [Abstract]

## Slide 183: Memory Systems and Memory-Centric Computing Systems Topic 2: Memory Reliability and Security
Prof. Onur Mutlu
omutlu@gmail.com
https://people.inf.ethz.ch/omutlu
9-13 July 2018
HiPEAC ACACES Summer School 2018

## Slide 184: Backup Slides

## Slide 185: More on DRAM Refresh

## Slide 186: Tackling Refresh: Solutions
Parallelize refreshes with accesses [Chang+ HPCA’14]
Eliminate unnecessary refreshes [Liu+ ISCA’12]
  Exploit device characteristics
  Exploit data and application characteristics
Reduce refresh rate and detect+correct errors that occur [Khan+ SIGMETRICS’14]
Understand retention time behavior in DRAM [Liu+ ISCA’13]

## Slide 187: Summary: Refresh-Access Parallelization
DRAM refresh interferes with memory accesses
  Degrades system performance and energy efficiency
  Becomes exacerbated as DRAM density increases
Goal: Serve memory accesses in parallel with refreshes to reduce refresh interference on demand requests
Our mechanisms:
  1. Enable more parallelization between refreshes and accesses across different banks with new per-bank refresh scheduling algorithms
  2. Enable serving accesses concurrently with refreshes in the same bank by exploiting parallelism across DRAM subarrays
Improve system performance and energy efficiency for a wide variety of different workloads and DRAM densities
  20.2% and 9.0% for 8-core systems using 32Gb DRAM at low cost
  Very close to the ideal scheme without refreshes
Chang+, “Improving DRAM Performance by Parallelizing Refreshes with Accesses,” HPCA 2014.

## Slide 188: Refresh Penalty
Processor
Memory Controller
DRAM
Refresh
Read
Data
Capacitor
Access transistor
Refresh delays requests by 100s of ns
Refresh interferes with memory accesses

## Slide 189: Existing Refresh Modes
Time
Per-bank refresh in mobile DRAM (LPDDRx)
Time
All-bank refresh in commodity DRAM (DDRx)
Bank 7
Bank 1
Bank 0
…
Bank 7
Bank 1
Bank 0
…
Refresh
Round-robin order
…
Per-bank refresh allows accesses to other banks while a bank is refreshing

## Slide 190: Shortcomings of Per-Bank Refresh
Problem 1: Refreshes to different banks are scheduled in a strict round-robin order
  The static ordering is hardwired into DRAM chips
  Refreshes busy banks with many queued requests when other banks are idle
Key idea: Schedule per-bank refreshes to idle banks opportunistically in a dynamic order

## Slide 191: Our First Approach: DARP
Dynamic Access-Refresh Parallelization (DARP)
  An improved scheduling policy for per-bank refreshes
  Exploits refresh scheduling flexibility in DDR DRAM
Component 1: Out-of-order per-bank refresh
  Avoids poor static scheduling decisions
  Dynamically issues per-bank refreshes to idle banks
Component 2: Write-Refresh Parallelization
  Avoids refresh interference on latency-critical reads
  Parallelizes refreshes with a batch of writes

## Slide 192: Shortcomings of Per-Bank Refresh
Problem 2: Banks that are being refreshed cannot concurrently serve memory requests
Time
Bank 0
RD
Delayed by refresh
Per-Bank Refresh

## Slide 193: Shortcomings of Per-Bank Refresh
Problem 2: Refreshing banks cannot concurrently serve memory requests
Key idea: Exploit subarrays within a bank to parallelize refreshes and accesses across subarrays
Time
Bank 0
Subarray 1
Subarray 0
RD
Subarray Refresh
Time
Parallelize

## Slide 194: Methodology
100 workloads: SPEC CPU2006, STREAM, TPC-C/H, random access
System performance metric: Weighted speedup
DDR3 Rank
Simulator configurations
Memory Controller
8-core processor
Memory Controller
Bank 7
Bank 1
Bank 0
…
L1 $: 32KB
L2 $: 512KB/core

## Slide 195: Comparison Points
All-bank refresh [DDR3, LPDDR3, …]
Per-bank refresh [LPDDR3]
Elastic refresh [Stuecheli et al., MICRO ‘10]:
  Postpones refreshes by a time delay based on the predicted rank idle time to avoid interference on memory requests
  Proposed to schedule all-bank refreshes without exploiting per-bank refreshes
  Cannot parallelize refreshes and accesses within a rank
Ideal (no refresh)

## Slide 196: System Performance
Chart: DRAM Chip Density
All-Bank | 5.5359 | 5.3024 | 4.8311
Per-Bank | 5.7551 | 5.5256 | 5.0271
Elastic | 5.6343 | 5.3803 | 4.8911
DARP | 5.9537 | 5.8162 | 5.2317
SARP | 5.9777 | 5.9152 | 5.7295
DSARP | 5.9723 | 5.9543 | 5.8059
Ideal | 6.0252 | 6.0252 | 6.0252
7.9%
12.3%
20.2%
1. Both DARP & SARP provide performance gains and combining them (DSARP) improves even more
2. Consistent system performance improvement across DRAM densities (within 0.9%, 1.2%, and 3.8% of ideal)

## Slide 197: Energy Efficiency
3.0%
5.2%
9.0%
Consistent reduction on energy consumption
Chart: DRAM Chip Density
All-Bank | 38.2974 | 40.28 | 44.8967
Per-Bank | 38.0134 | 39.9893 | 44.5521
Elastic | 37.5049 | 39.3169 | 44.1509
DARP | 37.191 | 38.5881 | 43.25
SARP | 37.1096 | 38.322 | 41.0809
DSARP | 37.137 | 38.197 | 40.8495
Ideal | 36.6284 | 36.6284 | 36.6284

## Slide 198: More Information on Refresh-Access Parallelization
Kevin Chang, Donghyuk Lee, Zeshan Chishti, Alaa Alameldeen, Chris Wilkerson, Yoongu Kim, and Onur Mutlu, "Improving DRAM Performance by Parallelizing Refreshes with Accesses" Proceedings of the 20th International Symposium on High-Performance Computer Architecture (HPCA), Orlando, FL, February 2014. [Summary] [Slides (pptx) (pdf)]

## Slide 199: Tackling Refresh: Solutions
Parallelize refreshes with accesses [Chang+ HPCA’14]
Eliminate unnecessary refreshes [Liu+ ISCA’12]
  Exploit device characteristics
  Exploit data and application characteristics
Reduce refresh rate and detect+correct errors that occur [Khan+ SIGMETRICS’14]
Understand retention time behavior in DRAM [Liu+ ISCA’13]

## Slide 200: Most Refreshes Are Unnecessary
Retention Time Profile of DRAM looks like this:

## Slide 201: RAIDR: Eliminating Unnecessary Refreshes
1. Profiling: Profile the retention time of all DRAM rows
2. Binning: Store rows into bins by retention time
 use Bloom Filters for efficient and scalable storage
3. Refreshing: Memory controller refreshes rows in different bins at different rates
 probe Bloom Filters to determine refresh rate of a row
1.25KB storage in controller for 32GB DRAM memory
Can reduce refreshes by ~75%
 reduces energy consumption and improves performance
Liu et al., “RAIDR: Retention-Aware Intelligent DRAM Refresh,” ISCA 2012.

## Slide 202: RAIDR: Baseline Design
Refresh control is in DRAM in today’s auto-refresh systems
RAIDR can be implemented in either the controller or DRAM

## Slide 203: RAIDR in Memory Controller: Option 1
Overhead of RAIDR in DRAM controller:
1.25 KB Bloom Filters, 3 counters, additional commands issued for per-row refresh (all accounted for in evaluations)

## Slide 204: RAIDR in DRAM Chip: Option 2
Overhead of RAIDR in DRAM chip:
Per-chip overhead: 20B Bloom Filters, 1 counter (4 Gbit chip)
Total overhead: 1.25KB Bloom Filters, 64 counters (32 GB DRAM)

## Slide 205: RAIDR: Results and Takeaways
System: 32GB DRAM, 8-core; SPEC, TPC-C, TPC-H workloads
RAIDR hardware cost: 1.25 kB (2 Bloom filters)
Refresh reduction: 74.6%
Dynamic DRAM energy reduction: 16%
Idle DRAM power reduction: 20%
Performance improvement: 9%
Benefits increase as DRAM scales in density

## Slide 206: DRAM Device Capacity Scaling: Performance
RAIDR performance benefits increase with DRAM chip capacity
Liu et al., “RAIDR: Retention-Aware Intelligent DRAM Refresh,” ISCA 2012.

## Slide 207: DRAM Device Capacity Scaling: Energy
RAIDR energy benefits increase with DRAM chip capacity
Liu et al., “RAIDR: Retention-Aware Intelligent DRAM Refresh,” ISCA 2012.

## Slide 208: RAIDR: Eliminating Unnecessary Refreshes
Observation: Most DRAM rows can be refreshed much less often without losing data [Kim+, EDL’09][Liu+ ISCA’13]
Key idea: Refresh rows containing weak cells
more frequently, other rows less frequently
  1. Profiling: Profile retention time of all rows
  2. Binning: Store rows into bins by retention time in memory controller
  Efficient storage with Bloom Filters (only 1.25KB for 32GB memory)
  3. Refreshing: Memory controller refreshes rows in different bins at different rates
Results: 8-core, 32GB, SPEC, TPC-C, TPC-H
  74.6% refresh reduction @ 1.25KB storage
  ~16%/20% DRAM dynamic/idle power reduction
  ~9% performance improvement
  Benefits increase with DRAM capacity
Liu et al., “RAIDR: Retention-Aware Intelligent DRAM Refresh,” ISCA 2012.

## Slide 209: More on RAIDR
Jamie Liu, Ben Jaiyen, Richard Veras, and Onur Mutlu, "RAIDR: Retention-Aware Intelligent DRAM Refresh" Proceedings of the 39th International Symposium on Computer Architecture (ISCA), Portland, OR, June 2012. Slides (pdf)

## Slide 210: Tackling Refresh: Solutions
Parallelize refreshes with accesses [Chang+ HPCA’14]
Eliminate unnecessary refreshes [Liu+ ISCA’12]
  Exploit device characteristics
  Exploit data and application characteristics
Reduce refresh rate and detect+correct errors that occur [Khan+ SIGMETRICS’14]
Understand retention time behavior in DRAM [Liu+ ISCA’13]

## Slide 211: Motivation: Understanding Retention
Past works require accurate and reliable measurement of retention time of each DRAM row
  To maintain data integrity while reducing refreshes
Assumption: worst-case retention time of each row can be determined and stays the same at a given temperature
  Some works propose writing all 1’s and 0’s to a row, and measuring the time before data corruption
Question:
  Can we reliably and accurately determine retention times of all DRAM rows?

## Slide 212: Two Challenges to Retention Time Profiling
Data Pattern Dependence (DPD) of retention time
Variable Retention Time (VRT) phenomenon

## Slide 213: An Example VRT Cell
A cell from E 2Gb chip family

## Slide 214: VRT: Implications on Profiling Mechanisms
Problem 1: There does not seem to be a way of determining if a cell exhibits VRT without actually observing a cell exhibiting VRT
  VRT is a memoryless random process [Kim+ JJAP 2010]
Problem 2: VRT complicates retention time profiling by DRAM manufacturers
  Exposure to very high temperatures can induce VRT in cells that were not previously susceptible
   can happen during soldering of DRAM chips
   manufacturer’s retention time profile may not be accurate
One option for future work: Use ECC to continuously profile DRAM online while aggressively reducing refresh rate
  Need to keep ECC overhead in check

## Slide 215: More on DRAM Retention Analysis
Jamie Liu, Ben Jaiyen, Yoongu Kim, Chris Wilkerson, and Onur Mutlu, "An Experimental Study of Data Retention Behavior in Modern DRAM Devices: Implications for Retention Time Profiling Mechanisms" Proceedings of the 40th International Symposium on Computer Architecture (ISCA), Tel-Aviv, Israel, June 2013. Slides (ppt) Slides (pdf)

## Slide 216: Tackling Refresh: Solutions
Parallelize refreshes with accesses [Chang+ HPCA’14]
Eliminate unnecessary refreshes [Liu+ ISCA’12]
  Exploit device characteristics
  Exploit data and application characteristics
Reduce refresh rate and detect+correct errors that occur [Khan+ SIGMETRICS’14]
Understand retention time behavior in DRAM [Liu+ ISCA’13]

## Slide 217: Towards an Online Profiling System
Key Observations:
Testing alone cannot detect all possible failures
Combination of ECC and other mitigation techniques is much more effective
  But degrades performance
Testing can help to reduce the ECC strength
  Even when starting with a higher strength ECC
Khan+, “The Efficacy of Error Mitigation Techniques for DRAM Retention Failures: A Comparative Experimental Study,” SIGMETRICS 2014.
Notes: Our high-level design for online profiling system is based to thee key observations:

## Slide 218: Towards an Online Profiling System
Run tests periodically after a short interval
at smaller regions of memory
Initially Protect DRAM
with Strong ECC
1
Periodically Test
Parts of DRAM
2
ECC
Test
Test
Test
Mitigate errors and
reduce ECC
3
Notes: Based on these observations, we propose that in an online profiling system,

## Slide 219: More on Online Profiling of DRAM
Samira Khan, Donghyuk Lee, Yoongu Kim, Alaa Alameldeen, Chris Wilkerson, and Onur Mutlu, "The Efficacy of Error Mitigation Techniques for DRAM Retention Failures: A Comparative Experimental Study" Proceedings of the ACM International Conference on Measurement and Modeling of Computer Systems (SIGMETRICS), Austin, TX, June 2014. [Slides (pptx) (pdf)] [Poster (pptx) (pdf)] [Full data sets]

## Slide 220: How Do We Make RAIDR Work in the Presence of the VRT Phenomenon?

## Slide 221: Making RAIDR Work w/ Online Profiling & ECC
Moinuddin Qureshi, Dae Hyun Kim, Samira Khan, Prashant Nair, and Onur Mutlu, "AVATAR: A Variable-Retention-Time (VRT) Aware Refresh for DRAM Systems" Proceedings of the 45th Annual IEEE/IFIP International Conference on Dependable Systems and Networks (DSN), Rio de Janeiro, Brazil, June 2015. [Slides (pptx) (pdf)]

## Slide 222: AVATAR
Insight: Avoid retention failures  Upgrade row on ECC error
Observation: Rate of VRT >> Rate of soft error (50x-2500x)
A
B
C
D
E
F
G
H
DRAM Rows
RETENTION
PROFILING
Weak Cell
0
0
1
0
0
0
1
0
Ref. Rate Table
ECC
ECC
ECC
ECC
ECC
ECC
ECC
ECC
1
AVATAR mitigates VRT by increasing refresh rate on error
Scrub
(15 min)
Row protected from future
retention failures

## Slide 223: RESULTS: REFRESH SAVINGS
AVATAR
No VRT
AVATAR reduces refresh by 60%-70%, similar to multi rate refresh but with VRT tolerance
Retention Testing Once a Year can revert refresh saving from 60% to 70%

## Slide 224: SPEEDUP
Speedup
Chart: 
| 8Gb | 16Gb | 32Gb | 64Gb
AVATAR (1yr) | 1.04 | 1.065 | 1.13 | 1.35
NoRefresh | 1.05 | 1.09 | 1.21 | 1.54
AVATAR gets 2/3rd the performance of NoRefresh. More gains at higher capacity nodes

## Slide 225: ENERGY DELAY PRODUCT
Chart: 
| 8Gb | 16Gb | 32Gb | 64Gb
AVATAR (1yr) | 0.95 | 0.88 | 0.75 | 0.52
NoRefresh | 0.91 | 0.83 | 0.68 | 0.41
Energy Delay Product
AVATAR reduces EDP,
Significant reduction at higher capacity nodes

## Slide 226: Making RAIDR Work w/ Online Profiling & ECC
Moinuddin Qureshi, Dae Hyun Kim, Samira Khan, Prashant Nair, and Onur Mutlu, "AVATAR: A Variable-Retention-Time (VRT) Aware Refresh for DRAM Systems" Proceedings of the 45th Annual IEEE/IFIP International Conference on Dependable Systems and Networks (DSN), Rio de Janeiro, Brazil, June 2015. [Slides (pptx) (pdf)]

## Slide 227: DRAM Refresh: Summary and Conclusions
DRAM refresh is a critical challenge
  in scaling DRAM technology efficiently to higher capacities
Discussed several promising solution directions
  Parallelize refreshes with accesses [Chang+ HPCA’14]
  Eliminate unnecessary refreshes [Liu+ ISCA’12]
  Reduce refresh rate and detect+correct errors that occur [Khan+ SIGMETRICS’14]
Examined properties of retention time behavior [Liu+ ISCA’13]
  Enable realistic VRT-Aware refresh techniques [Qureshi+ DSN’15]
Many avenues for overcoming DRAM refresh challenges
  Handling DPD/VRT phenomena
  Enabling online retention time profiling and error mitigation
  Exploiting application behavior

## Slide 228: End of Backup Slides